        Technical Data

Description:
 API glass tile is classified by the Tile Council of North America as large format, low-temperature-coated, standard grade glass tile. The aesthetic class is VO meaning “very uniform in appearance and smooth in texture”. The thickness is 6mm and the weight is three pounds per square foot. Not recommended for floor tile installations. API glass tiles are suitable for interior and exterior applications; both commercial and residential. Rated “impervious” glass tiles are frost proof, resistant to chemical attack, resistant to fading and discoloration, and impervious to water and most stains. For complete installation instructions contact the API Customer Service Department at (336) 877-6951

 References:
American Society for Testing and Materials (ASTM)
ASTM C499 ASTM C485 ASTM C502 ASTM C1378
ASTM C424 ASTM C650 ASTM C609 ASTM C1026
ASTM C373 ASTM C372 ASTM C920 ASTM C1027
American National Standards Institute (ANSI)
ANSI A108.6 ANSI A137.2 ANSI A108.01 ANSI A108.02
Tile Council of North America (TCNA) Handbook-latest edition

   ANSI A-137.2
        Property Required Achieved
Nominal size (ASTM C499) -2.00 - +2.00% .001%
Caliber range (ASTM C499) -0.3 - +0.3% .003%
Thickness (ASTM C499) range 0.031in. 0.001in.
Warpage – edge (ASTM C485) -0.3 - +0.4 % 0.003%
Warpage-diameter (ASTM C485) -0.3 - +0.4 % 0.0035%
Wedging (ASTM C502) -0.25 - +0.25% 0.015%
Water absorption (C373) n/a Impervious
Crazing resistance (C424) pass n/a
Bond strength (section 7.7 epoxy set) 150 psi 475 psi
Chemical resistance (ASTM 650) n/a A (no affect)
Freeze/thaw (ASTM 1026) n/a Pass
Stain resistance (ASTM 1378) n/a A (no affect)
Color uniformity (ASTM C609) n/a VO- very uniform
Abrasion resistance (ASTM C1027) n/a 0
        (not designated for floors)

  PART TWO – INSTALLATION INSTRUCTIONS

Note: The Tile Council of North America states that mortars specifically formulated or recommended for glass tile must be used. Some low-temperature-coated glass tiles are not intended for installation with cementitious materials,as cement mortar alkalinity may deteriorate the tile backing and cause delamination.

Approved Methods:
Approved wall tile installation methods include all Tile Council of North America methods found in the TCNA Handbook for Ceramic, Glass, and Stone Tile Installation with the exceptions of Methods W215, W222, and W260. These three details which depict spot-bonding and one-coat mortar bed methods are not approved.
Approved Bond Coats
The bond coat MUST BE the specially formulated 100% solids “Epoxy Plus” mortar manufactured by Texrite, recommended by Andrew Pearson Industries, and made available by Piedmont Innovative Products Distributors located in Burlington, North Carolina and by all Daltile locations nationwide. This tile setting epoxy mortar conforms to all provisions of ANSI A118.3 and ISO 13007-R1T. It is available in eighteen colors.
In some instances Texrite Bondrite 1002 mastic may be used for tiling over interior dry areas with substrates such as drywall, however there are no systems warranties available for mastic applications.
All installations must conform to ANSI A108.6. All provisions of ANSI A108.01 and A108.02 are a part of the A108.6 standards.
Approved Grouts:
“Epoxy Plus” 100% solids epoxy grout by Texrite is approved. Conforms to ISO RG and is available in the same 18 colors as the bond coat. Also approved is Texrite Chromaflex resin based grout. Crack resistant and flexible it also repels stains and water. Cement free Chromaflex comes pre-mixed and ready to use. Follow detailed individual product directions.
Movement joints:
 Because glass expands more than ceramic tile, more movement accommodation may be needed. In every instance, the architect or designer shall show the specific locations and details of movement joints on project drawings. All perimeter and field movement joints shall conform to TCNA -EJ171 details.
Sealants:
Sealants for movement joints shall be either silicone or urethane Type S or M, Grade NS, Class 25 and 12-1/2, and Uses M&G complying with ASTM C920. Install movement joints per ASTM C1193 Standard Guide for Use of Joint Sealants.

Crack Isolation Membranes:
Glass tile is generally more vulnerable to crack propagation emanating from substrates than ceramic tile. Because of this it may be advisable to specify an ANSI A118.12 crack isolation membrane for large format glass tiles. API recommends and approves Texrite Hydro-Rite which is a liquid applied waterproofing and crack isolation membrane product which can be obtained from Piedmont Innovative Products. Texrite Hydro-Rite can be applied via brush, roller, or trowel and comes in either 1,2, or 5 gallon containers. Two coats is advisable. Coverage should average 70-80 sq.ft. At 1/32”. Follow detailed product directions.
Water Proof Membranes:
When waterproof membranes are needed API recommends the same Texrite Hydro-Rite product as is listed under crack isolation membranes. Complies with ANSI A118.10. Two coats are required reaching a combined total thickness of 3/64” to 1/8”. Two coat wet coverage should be 35 - 40 sq.ft. per gallon. Follow detailed product directions.
Surface Prep Products:
Note: The API “Bright & Bold Collection” of tiles are not designated for floors due to low abrasion resistance and low co-efficient of friction, however if ever residentially installed the following surface prep products are suggested when needed to level or smooth horizontal surfaces: (select)
Screed 125 FS is a trowelable sanded cement based screed application covering 0” - 1'2”
Screed 375 system is a two part underlayment system covering 1/8” - 1-1/2”
Flowrite 250 is a high strength self leveling compound that may be applied in multiple pours of 1” each. Texrite Bonding Primer 500 will be needed to prime all substrates. Flow Rite 250 is intended for interior use only. Coverage will average 50-55- sq.ft. Per 50 pound bag. Bonding primer 500 diluted per instructions will cover 250 – 300 sq.ft. Of smooth concrete. Rough textured or absorptive surfaces will reduce coverage rates.
Tile Council of North America approved floor installation methods are F-116E, F-205 & 205A, F-131, F-132, F-134, F-141, F-143, F-144, F-145, F-185.
Warranty:
Andrew Pearson Industries (API) through it's installation materials partner offers a 20 year 100% labor and materials system warranty for all epoxy set wall tile installations. All prep, membrane, setting, and grouting products must be from the approved list outlined above. Manufacturer's instructions are to be followed in every instance. For a copy of the printed warranty document please contact the API Customer Service Department. For installation questions contact the API Customer Service Department.

API CUSTOMER SERVICE PIEDMONT INNOVATIVE PRODUCTS
(336) 877-6951 (336) 675-5887